## Slide 1
In House Quality Concern
Crack in Worm Shaft
Reni Cherian | Naresh Gauba | Yogesh
Approved By | Reviewed By | Prepared By

## Slide 2
Defect Detail | 
Part Name | Worm Shaft
Model effected | Y17, YHB 25MC, YXA 26MC & YTA (part is common)
Qty | N=6 part
Defect | Crack observed
Detected at | After Whirling process (100% visual inspection)
Detected by | Line Operator
Occurrence Date | 08.09.26
Material grade | SCM 435
NG Part
OK Part
1
PROBLEM DETAIL
SUPPLY CHAIN
XXXX
(RM Supplier)
XXXX
(Heat Treatment )
XXXX
(Machining)
XXX
(Machining)
XXXX
(CEPS ASSY)

## Slide 3
Item | Summary
Problem | Worm shaft crack detected during visual inspection at JIN Bawal . Total 6 NG parts identified (2 machining level + 4 child parts).
Containment | 100% magnifying glass inspection at JIN receiving & machining. 200% MPI implemented at Dynamic. Suspected stock segregated and under control.
Customer Impact | No performance difference observed between OK & NG parts in C-EPS evaluation. Reliability impact under validation.
Traceability | Suspected heat identified as M215871. Complete supply chain traced: Mukand → Omega → Dynamic → JIN.
XXXX Findings | SEM, microstructure and joint analysis did not confirm RM abnormality. Current evidence points towards heat-treatment related crack generation.
Supplier Position | Mukand /Omega have not confirmed raw material responsibility. Investigation and FTA validation are continuing.
XXXX Concern | Actual crack generation mechanism remains unproven. Occurrence root cause and permanent countermeasure not yet validated.
Outflow Root Cause | MPI visual inspection weakness identified. WI non-adherence, operator fatigue, inspection guideline gaps and inadequate monitoring suspected.
Current Status | Containment completed. Traceability completed. Joint supplier analysis completed. SEM review completed. Durability test and FTA validation in progress.
Open Points | Final occurrence root cause pending. Heat-treatment mechanism not validated. Durability test not completed. Supplier final report pending. Permanent countermeasure pending.
Supplier Commitment | Final investigation report from Mukand /Omega. FTA validation and technical conclusion submission.
Management Support Required | Continue escalation with Mukand /Omega management. Obtain technically validated root cause, countermeasure and closure evidence before concern closure.
2
Current Status, Key Findings & Open Issues

## Slide 4
3
Containment Action
Temporary Action:- Segregation at JIN BWL & Dynamic
Refer next slide for Segregation Detail and Method
Location | Model | Part level | Total Qty | OK | NG | Pending | Segg. Method | Picture
BWL Line | Y17 | Machining | 192 | 190 | 02 | 0 | 100% parts checking with Magnifying Glass -at Receipt stage - after whirling process - 08.09.26 200% MPI started at Dynamic - 08.09.26 | 
BWL (Receipt.) | Y17 | Child part | 4908 | 4904 | 04 | 0 |  | 
Dynamic (Child Parts) |  | Child part | 1105 | 1102 | 0 | 0 |  | 
Total |  |  | 6205 | 6199 | 6 | 0 |  | 
Confirmation Marking on Worm Shaft
(Receiving Stage-JIN)

## Slide 5
200% parts inspection by MPI
100% parts checking by Magnifying Glass (JIN RECEIVING STAGE)
100% parts checking by Magnifying Glass
Identification of containment-Identification Tag
IDENTIFICATION AFTER CONTAINMENT ACTIONS
Black Line Marking
3.1
Containment Action
AFTER WHIRLING-INSPECTION -JIN PRODUCTION LINE
Zoom View
Dynamic

## Slide 6
4
4M CHANGE
4M | Observation | Result
Man | Skilled | OK
Machine | No change | OK
Material | No change | OK
Method | As per work Instruction | OK
4M | Observation | Result
Man | Skilled | OK
Machine | No Change | OK
Material | No change | OK
Method | As per work Instruction | OK
MUKAND
4M | Observation | Result
Man | Skilled | OK
Machine | No change | OK
Material | No change | OK
Method | As per work Instruction | OK
Inference:-
- As per 4M change record
no abnormality observed
OMEGA
DYNAMIC

## Slide 7
5
PROCESS FLOW WITH DEFECTIVE PROCESS
Mini Blast Furnace
Energy Optimizing Furnace
Ladle Refining Furnace
Vacuum Degassing
Continues Casting
Billet Dressing
Hot Rolling to Desired Size & Shape
Bar Inspection
Dispatch
Mukand Process Flow
Omega Process Flow
Receiving inspection of RM
Straightening @ Ø19 mm
Peeling @ Ø18mm
Straightening @ Ø18mm
Hardening & Tempering
Pickling / Pointing / Cold Draw/ Pointing cutting @ Ø17.30mm
Straightening
Centre Less grinding 1
Centre Less grinding 2 (Final Size Ø17.00-0.04mm)
Inspection, Packing & Dispatch
Dynamic Process Flow
RM Receiving & Inspection
Turning & Cantering at Sliding Head
Dia. Turning
Crack Detection at MPI
Visual Inspection & Gauging
Packing & Dispatch
Occurrence
Outflow
Supplier Chain |  |  |  |  |  |  |  | 
Supplier → | Mukand |  | Omega |  | Dynamic |  | JIN BWL | 
Process → | Raw Material |  | Heat Treatment |  | Machining |  | Whirling | CEPS Assembly

## Slide 8
5.1
BAWAL-MACHINING PROCESS FLOW
RM Receiving & Inspection
Thread Cutting
Thread Grinding
Thread Grinding
OD Grinding
Washing
Space Runout
100% Visual inspection with Magnifying glass
LOWER SHAFT WASHING
R/G ANNEALING
DMC MARKING(WORM HOUSING)
W/H BEARING & C- RING PRESS IN
WS BEARING & FLANGE BOSS PRESS-IN
ABLS ASSY
ASSY MEASUREMENT
SQUARE RING ASSEMBLY & END COVER PRESS
DMC MARKING(LOWER SHAFT)
R/G PRESS
RED.GEAR TEETH CUTTING
REDUCTION GEAR DEBURRING
L/S BUSH AND BEARING PRESS
MAGNETIZING
'LOWER SHAFT ASSY INSTALLATION & C-RING PRESS
TOOTH SURFACE FORMING
RED.GEAR SPACE RUNOUT
Bawal Worm Housing Process Flow
Bawal Column Process Flow
DMC CODING (M/S)
DMC CODING (M/S)
TORSION BAR AND MIDDLE SHAFT PRESS
NEEDLE BEARING PRESS & MCR ATTACHMENT
MAGNETIC YOKE PRESS
GENERAL ASSEMBLY
OUTER JACKET PRESS
JACKET/LOWER TUBE PRESS
BUSH & COLLAR PRESS
GAP REGULATION, BALANCING & DEBURRING
N-MIN TORQUE INSPECTION
GAIN OFFSET WRITING & FIXED LOAD INSPECTION
MCU INSTALLATION
PROPORTIONAL LOAD INSPECTION
FEELING INSPECTION
TILT & TELESCOPICE INSPECTION
HARNESS BRACKET ATTACHMENT
PEDAL BRACEKET ATTACHMENT
MID POINT CURRENT & ROTATIONAL TORQUE INSPECTION
DIAG INSPECTION
IMS ATTACHEMENT
FINAL INSPECTION
CABLE TIE ATTACHMENT
BAWAL PROCESS FLOW
Detected at Process

## Slide 9
6
ANALYSIS
1. OK & NG PART COMPARISON DONE FOR MICROSTRUCTURE AT OMEGA
OK PART MICROSTRCTURE
NG PART MICROSTRCTURE
Inference:-
- No Decarb observed at Crack Portion.
- Tempered Martensite structure observed
2. OK & NG PART COMPARISON DONE FOR MICROSTRUCTURE AT JBIN
Inference:-
- Tempered Martensite structure observed
- RM Level issue not suspected
3. SEM TESTING PROCEED AT NG PART LEVEL
Inference:- As per SEM Testing Conclusion, No abnormality Observed at RM Level

## Slide 10
6.1
ANALYSIS
FTA SHARED BY THE OMEGA CONSIDERING THE POSSIBLE CAUSES
Inference:- Current Controls Verified by the Omega & Dynamic jointly And No Abnormality Observed.
JIN CQA & Plant QA will plan for the Validation Activities at Omega by 24rd Sep’26

## Slide 11
S.N. | Ideal Condition | Actual Condition | Factors
1 | Start of Machine | Follow as per the Work Instruction | Non-Significant
2 | Machine parameter setting | Follow as per the Work Instruction and PCS | Non-Significant
3 | Part Loading | Follow as per the Work Instruction | Non-Significant
4 | Start the process | Follow as per the Work Instruction | Non-Significant
5 | Part Unloading | Follow as per the Work Instruction | Non-Significant
6 | Visual Inspection at MPI | During inspection, hold the part at an angle of approximately 45 degrees and rotate it twice in both the forward and backward directions. | Non-Significant
7 | Demagnetization and sent to 100% Gauging | Follow as per the Work Instruction and PCS | Non-Significant
8 | Operator Concentration and Attention | ❶ Operator fatigue observed due to continues inspection under UV light for complete shift (shift is of 11 working hours) | Significant
9 | Visual Inspection at Final Stage | ❷ Only general guidelines for inspection available. Part specific guidelines considering sequential check points for inspection at Final inspection stage. | Significant
Process verification of MPI
- Why out flow from Dynamic
Action Planned.
❶ MPI operator to be changed / rotated every 04 hours - 10.09.26 (Started)
❷ Final inspection guidelines to be changed for specific crack identification - 12.09.26 (Started)
6.2
ANALYSIS

## Slide 12
6.3
ACTIVITY PLAN & STATUS
ACTIVITY PLAN |  |  |  |  | 
S.No | Activity Defined | Resp | T.Date | Status | Remarks
1 | Dynamic is doing 200% MPI for crack detection | Ravi Bajwa | 08.09.26 | Started | Still no no NG observed
2 | AT JIN Bawal Receiving stage, 100% confirmation visually with magnifying glass | Naresh Gauba | 08.09.26 | Started | Still no no NG observed
3 | After Whirling process, 100% visual confirmation with magnifying glass | Rakesh Nain | 08.09.26 | Started | Still no no NG observed
4 | Assemble NG worm shaft in C-EPS and performance results to be confirmed(Comparison of Ok & NG Assy) | Rakesh Nain | 09.09.26 | Done | Performance results observed OK on production line
5 | Comparison of Micro-structure And Hardness Inspection of Ok & NG Part at JIN | Naresh Gauba & Yogesh San | 12.09.26 | Done | Structure Observed-Tempered Martensite . - RM Level issue not suspected*
6 | Comparison of Micro-structure And Hardness Inspection of Ok & NG Part at Omega | Omega+Dynamic | 12.09.26 | Done | 
7 | CEPS assembly with one crack worm shaft send to JIN TC for reducer durability testing | Kamal San/Praveen San-JIN GGN LAB | Oct’26 (4th Week) | Started | 
8 | Investigation Report to be Received from Mukand of the NG Part. (As per Action plan, Mukand is proceeding for the testing) | Omega/Dynamic | 24.09.26 |  | 
09 | Simulation activities to be done based on FTA at Omega | Yogesh-CQA/Naresh Gauba-QA | 24.09.26 |  | 
10 | Outflow Root Cause and Permanent Actions to be Shared | Dynamic | 25.09.26 |  | 

## Slide 13
7
Challenges being faced during analysis
1. Both Raw material supplier XXXX & Heat treatment supplier XXX
not ready to accept the defect occurrence at their end
(as per expert – this defect can be occurred during heat treatment (at XXX)
Facing difficulty in coordinating with all the 03 suppliers for analysis.

## Slide 14
Thank You

## Slide 15
Suspected Quantity
WORM SHAFT CRACK PART TRACEABILITY DETAIL (SUSPECTED HEAT CODE-M215871) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Mukund to Omega |  | OMEGA Process |  |  |  |  |  |  |  | DYNAMIC |  |  |  |  |  | JIN BAWAL |  |  | Remarks | 
 |  | IMT Faridabad Plant |  |  | Sector 24 Plant |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Date | A Qty | Heat Treatment & Peeling Date (HT) | B Peeling + HT Qty (KG) | C Scrap Qty (KG) | Pickling + Drawing + Grinding Date | Pickling + Drawing + Grinding Qty | D Scrap Qty | E OK Qty | Remaining A-(B+C+D+E) | Received Date | Recd Qty | Dynamic Production Data | Dynamic Rej Data | Dynamic Despatch to JIN | Opening Qty for next month | JIN Receiving Month/Date | CEPS Despatch Date | C-EPS Despatch QTY |  | 
 | In KG |  | In KG | In KG |  | In KG | In KG | In KG | In KG |  | In KG | In Nos | In Nos | In Nos | In Nos |  |  | In Nos |  | 
Heat-M215871-First Receiving 14.05.2026 | 12600 | 23.05.2026 | 3820 | 1380 | 25.05.2026 | 1820 | 146 | 1674 | 0 | 28.05.26 | 920 | 31908 | 154 | 25700 | 6054 | Jun'26 | -- | -- |  | 
 |  |  |  |  | 26.05.2026 | 2000 | 160 | 1840 |  | 02.06.26 | 2680 |  |  |  |  |  |  |  |  | 
 |  | 27.05.2026 | 7400 |  | 27.05.2026 | 3000 | 240 | 2760 |  | 04.06.26 | 2550 |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 29.05.2026 | 1400 | 112 | 1288 |  | 17.06.26 | 4130 |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 30.05.2026 | 3000 | 240 | 2760 |  | 02.07.26 | 1010 | 42811 | 167 | 45700 | 2998 | Jul'26 | -- | -- |  | 
20.06.2026 | 3140 | 27.06.2026 | 2810 | 330 | 29.06.2026 | 1200 | 96 | 1104 | 0 | 08.07.26 | 1460 |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 30.06.2026 | 1610 | 129 | 1481 |  | 18.07.26 | 1270 |  |  |  |  |  |  |  |  | 
01.07.2026 | 6280 | 08.07.2026 | 5580 | 700 | 13.07.2026 | 1200 | 96 | 1104 | 0 | 28.07.26 | 4050 |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 14.07.2026 | 800 | 64 | 736 |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 15.07.2026 | 1500 | 120 | 1380 |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 16.07.2026 | 1000 | 80 | 920 |  | 13.08.26 | 900 | 46464 | 189 | 46800 | 2473 | Aug'26 | -- | -- |  | 
 |  |  |  |  | 17.07.2026 | 1080 | 86 | 994 |  |  |  |  |  |  |  |  |  |  |  | 
31.07.2026 | 8970 | 08.08.2026 | 2690 | 870 | 09.08.2026 | 800 | 64 | 736 | 0 | 18.08.26 | 1420 |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 10.08.2026 | 1500 | 120 | 1380 |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  | 11.08.2026 | 390 | 31 | 359 |  |  |  |  |  |  |  |  |  |  |  | 
 |  | 17.08.2026 | 2730 |  | 20.08.2026 | 1300 | 104 | 1196 | 0 | 27.08.26 | 2110 | 8461 | 29 | 2000 | 1005 | 01-Sep-26 | 05.09.2026 | 1740 | > From 05th to 08th of Sep, Suspected lot despach to customer. - Total dispatch to customer - 4800 (out of 5649 nos, 849 is with other heat material) | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 300 |  | 01-Sep-26 | 06.09.2026 | 750 |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1700 |  | 02-Sep-26 | 07.09.2026 | 1414 |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 700 |  | 03-Sep-26 | 08.09.26 | 1745 |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 300 |  | 03-Sep-26 |  |  |  | 
 |  |  |  |  | 21.08.2026 | 1430 | 114 | 1316 |  |  |  |  |  | 1300 |  | 06-Sep-26 | -- | -- |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1200 |  | 06-Sep-26 |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 700 |  | 08-Sep-26 |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1700 |  | 08-Sep-26 |  |  |  | 
 |  | 20.08.2026 | 2680 |  | 22.08.2026 | 1800 | 144 | 1656 |  | 01.09.26 | 1250 | -- | -- | -- |  | -- |  |  | Not Consumed | 
 |  |  |  |  | 24.08.2026 | 880 | 70 | 810 |  |  |  |  |  |  |  |  |  |  |  | 
Total | 30990 |  | 27710 | 3280 |  | 27710 | 2216 | 25494 |  |  | 23750 | 129644 | 539 | 128100 |  |  |  | 4800 |  | 
 |  |  |  |  |  |  |  |  |  |  | Pending at Dynamic-FG Qty |  |  |  |  | 1005 Nos | Till 08th of Sep'26 |  |  | 
 |  |  |  |  |  |  |  |  |  |  | Pending Material at RM Stage(Dynamic) |  |  |  |  | 1250 KG |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  | Pending at Omega End (Ok Qty at Omega-Total Received at Dynamic) |  |  |  |  | 1744 KG |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Receiving of Last Suspected lot at Omega |  |  |  |  | 31.07.26
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Received at Dynamic End |  |  |  |  | 27.08.26
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Received at JTEKT |  |  |  |  | 03.09.26
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Dispatch to Customer |  |  |  |  | 05.09.26 to 08.09.26